## Slide 1: dr. Zsuzsanna Gaál-Szabó, head of company, Energochem Ltd., Hungary Examination of lifetime of railway transformers
INNORAIL 2015
zsuzsagsz@gmail.com

## Slide 3
Lifetime of transformer =
Lifetime of insulating paper

## Slide 4
Mass of paper and oil in transformer
Chart: 
| paper | oil
 | 10 | 200

## Slide 7
.

## Slide 8
Thermally overstressed insulation
Paper deterioration by overheating

## Slide 10
(source: CIGRE A2-445, 2011)
Influence of temperature combined with water on solid insulation life time
(Laboratory experiment on a Kraft paper sample)

## Slide 11
“strategic” end-of-life
“economical” end-of-life
End-of-life criteria should be associated with a higher risk of transformer failure

## Slide 12
Normal insulation life of a well dried, oxygen free, thermally upgraded insulation system, at the reference temperature 110°C (IEC 60076-7:2005)

## Slide 13
Life of paper under various conditions (IEC 60076-7:2005)

## Slide 16
(Source: CIGRE D1-111, 2012)
Typical correlation between tensile strength and degree of polymerization value for Kraft paper
Diagnostics from paper: measurement of the average viscometric degree of polymerization
Degree of polymerization
Degree of polymerization

## Slide 17
(Source: CIGRE A2-102,2014)

## Slide 18
(Source: CIGRE A2-106,2014)

## Slide 19
Typical correlation between degree of polymerization and furan content
(Source: CIGRE D1-494, 2012)
Diagnostics from oil: furan analysis
DP: degree of polymerization
2FAL: 2-furfural

## Slide 20
(source: CIGRE A2-107,2014)

## Slide 21
(Source: CIGRE A2-445, 2011)

## Slide 22
Diagnostics
in practice

## Slide 23
Simulation of maintenance action of cellulosic insulation and its effect on retarding ageing.
(source: CIGRE D1-323, 2007)

## Slide 24
Lifetime of Kraft paper
…without maintenance
….with maintenance

## Slide 26: Thank you for your attention!
INNORAIL 2015
zsuzsagsz@gmail.com